## Slide 1: DEVELOPMENT OF THE METHOD FOR DETERMINING THE HEAVY ION CHARACTERISTICS USING SOLID-STATE DETECTORS (GLASS, MINERALS)
Starkova E.N., Polukhina N.G., Starkov N.I., Konovalova N.S.,
Okateva N.M., Chernyavskiy M.M., Shchedrina T.V.
In the Laboratory elementary particles (LPI) during many years
solid-state detectors are used (glasses, minerals, plastics)
1. Determination of nuclear charge in olivine from meteorites
Glass Olivine Plastic
Meteorites Epoxy PAVICOM Nuclear track
The measured values are track length L and etching rate V. The connection Z(L,V) is necessary
Calibration five-parameter Surface Z(L,V) charge distribution experiments function of galactic nuclei
2. Determination of charge and energy of nuclei
This method is continuation of that used in olivine investigation : Track length, etching rate => Charge, energy Several samples were exposed with three nuclei and now they are in processing.
=> The model experiment was carried out (The SRIM calculations of L(Z,E)+our results about V(Z,E) )
L, мм | V/100, мкм/ч | Z/100 |  | Энергия E, Мэв/1000 | 
 |  | Реальный | Оценка | Реальная | Оценка
0,05421 | 0,2207 | 0,54 | 0,537375 | 0,09 | 0,08932
0,07664 | 0,266 | 0,54 | 0,536125 | 0,13 | 0,1286
0,03847 | 0,1522 | 0,46 | 0,45875 | 0,05 | 0,04972
0,05796 | 0,1923 | 0,46 | 0,45875 | 0,08 | 0,07884
0,05397 | 0,1416 | 0,36 | 0,360125 | 0,055 | 0,05437
0,06898 | 0,1596 | 0,36 | 0,3584375 | 0,07 | 0,06902
0,05223 | 0,09877 | 0,26 | 0,2656875 | 0,0375 | 0,03658
0,08268 | 0,1205 | 0,26 | 0,260125 | 0,055 | 0,05409
0,06476 | 0,07047 | 0,18 | 0,1816875 | 0,0275 | 0,02787
0,09656 | 0,08312 | 0,18 | 0,1804375 | 0,0375 | 0,03783
Approximating function:
V=A(Z)+B(Z)*L+C(Z)*L*L
Ar Kr Xe
A(Z) B(Z)r C(Z)
3. Stability of nuclei tracks at high temperature in solid-detectors.
Such conditions arise in experiments on synthesis of superheavy elements.
1 The tracks disappear (C48-3).
2 The tracks are kept but change their characteristics (KУ-2, KNFS-3, SELG).
3 The tracks are retained their characteristics (Indian mica).
The classification of the solid-state detector by stability to temperature
Indian mica irradiated
by Bi of 670 MeV
Normal Annealing for hours
conditions at 500 degrees
The work was supported by a grant from the Russian Science Foundation 23-12-00054
Lebedev Physical Insitute